Edinburgh Napier University

Quantum Dots:  An investigation into how differing surface characteristics affect their interaction with macrophages in vitro

Martin James David Clift

Doctorate of Philosophy

2008

ABSTRACT

Quantum dots (QDs) are potentially advantageous tools for both diagnostics and therapeutics due to their light emitting characteristics.  The impact of QDs on biological systems however, is not fully understood.  The aim of this project therefore, was to investigate the interaction of a series of different surface modified QDs with macrophages and their subsequent toxicity.  CdTe/CdSe (core), ZnS (shell) QDs with either an organic, COOH or NH2 polyethylene glycol (PEG) surface coating were used.  Fluorescent COOH polystyrene beads (PBs) at (Ø) 20nm and 200nm were also studied.  J774.A1 murine ‘macrophage-like’ cells were treated for two hours with QDs (40nM) or PBs (50μg.ml-1) in the presence of 10% FCS prior to assessment of cellular uptake via confocal microscopy and flow cytometry.  COOH and NH2 (PEG) QDs, as well as 20nm and 200nm PBs entered macrophages within 30 minutes, and were found to locate within endosomes, lysosomes and the mitochondria.  T.E.M. also illustrated particles, including organic QDs, to be present inside J774.A1 cells within membrane-bound vesicles at two hours.  Organic QDs were unable to be visualised via fixed cell confocal microscopy.  Live cell confocal microscopy (without 10% FCS) did suggest however, that organic QDs entered cells in low quantities up to 30 minutes, after which fluorescence declined.  Particle toxicity was determined over 48 hours via the MTT, LDH and GSH assays, as well as via assessment of their potential to produce the pro-inflammatory cytokine TNF- and effect cytosolic Ca2+ signalling in J774.A1 cells.  Organic QDs were found to be highly toxic at all time points and concentrations used.  Both COOH QDs and NH2 (PEG) QDs induced significant (p<0.0001) cytotoxicity (MTT and LDH assays) at 80nM after   48 hours, as well as significant (p<0.01) GSH depletion over 24 hours at all doses, as well as increasing the level of cytosolic Ca2+ at 40nM when assessed over 30 minutes.  Organic and NH2 (PEG) QDs were found to significantly increase TNF- production after 24 hours at 80nM.  The findings of this study demonstrate that QDs differ in their uptake by macrophages according to their surface coating, with the organic surface coated QDs being the most toxic. At sub-lethal concentrations, in the presence of 10% FCS, the COOH and NH2 (PEG) QDs are taken up resulting in GSH depletion and modulated Ca2+ signalling, with NH2 (PEG) QDs and organic QDs only eliciting limited TNF- production.  Interestingly however, despite these observations, QD surface coating does not affect the intracellular fate of these NPs, with all of the different surface coated QDs observed to be present within endosomes, lysosomes and the mitochondria within J774.A1 macrophage cells.  Therefore, in conclusion, the surface coating of QDs plays a significant role in their interaction with macrophages, their uptake and their subsequent toxicity.

In loving memory of

Eric Stanley Dickinson

“Uncle Eric”

When you know a thing, to hold that you know it; and when you not know a thing, to allow that you do not know it

– this is knowledge

The Confucian Analects

Confucius (551 BC – 479 BC)

CONTENTS

Section								        Page

1. Chapter One: Introduction 						1

1.1 Nanotechnology							1

1.2 NPs									4

1.2.1 Accidental NPs						4

1.2.2 Engineered NPs						4

1.2.3 Applications of Engineered NPs				6

1.3. NP Toxicology – A Historical Perspective 			7

1.4 Potential Exposure Routes of NPs					13

1.5 The Macrophage cell							17

1.5.1 Structure and Function of the Macrophage Cell		17

1.5.2 Cellular Uptake 						19

1.5.2.1 Passive Cellular Uptake				19

1.5.2.2 Active Cellular Uptake				20

1.6 NP Toxicity - The oxidative stress paradigm			22

1.6.2 NP Toxicity - Cell Death					29

1.6.2 NP Toxicity and Macrophage cells				30

1.7 Nanomedicine								31

1.8 QDs									33

1.8.1 Structure of QDs						33

1.8.2 Polymer Coatings						34

1.8.3 Bioimaging characteristics of QDs				36

1.8.4 Cd Toxicity							38

1.8.5 QD Toxicity							39

Section								        Page

1. Chapter One: Introduction (continued)

1.8 QDs (continued)

1.8.6 Fate of QDs							43

1.9 Aim of Project								45

2. Chapter Two: General Methods					47

2.1 Chemicals and Reagents						48

2.2 Cells 									48

2.2.1 J774.A1 Cells 							48

2.2.2 J774.A1 Cell Culture						48

2.2.3 J774.A1 Cell Sub-culture					48

2.3 Particles									48

2.3.1 QDs								48

2.3.2 PBs								49

2.4 Particle Preparation							51

2.5 Cytotoxicity of Particles						51

2.5.1 MTT Assay							51

2.5.2 LDH Assay							53

2.6 Statistical Analysis							54

Section								        Page

3. Chapter Three:								55

‘The impact of different nanoparticle surface chemistry and size on uptake, stability and toxicity in a murine macrophage cell line’

3.1 Introduction								56

3.2 Materials and Methods						58

3.2.1 Cellular Uptake of Particles				58

3.2.1.1 Fixed Cell Analysis – Cell Preparation 		58

and Fixation

3.2.1.1.1 Immunofluorescent Staining and 	58

Fixed Cell Imaging

3.2.1.1.2 Restoration of Z-stack images		60

3.2.1.1.3 Effects of Trypan blue on 		60

J774.A1 cell viability

3.2.1.1.4 Investigation of the potential for 	61

non-specific binding of cytoskeleton

tubulin antibodies to J774.A1

macrophage cells

3.2.1.2 Live Cell Imaging					62

3.2.1.2.1 Live Cell Imaging -                               64

Amended Protocol

3.2.1.3 Cellular Fluorescence via Flow Cytometry	65

3.2.2 Fluorescent Stability of Particles			68

3.2.2.1 Fluorimeter slit-width				68

3.2.3 Particle Size							69

3.2.4 Exocytosis of Particles					70

3.2.4.1 Exocytosis Adsorption Control			71

Section								        Page

3. Chapter Three (continued):

3.2.5 Cytotoxicity of Particles					71

3.2.5.1 MTT Assay 						71

3.2.5.2 LDH Release					72

3.2.5.2.1 LDH Adsorption					72

3.2.6 Statistical Analysis						73

3.3 Results									74

3.3.1 Cellular Uptake of Particles assessed 			74

via Confocal Microscopy

3.3.1.1 Fixed cell imaging					74

3.3.1.2 Live cell imaging of QDs				86

3.3.1.2.1 Live cell imaging of PBs			91

3.3.1.3 Cellular Fluorescence assessed via 		94

Flow cytometry

3.3.2 Fluorescent stability					97

3.3.3 Particle size							102

3.3.4 Exocytosis of NPs						103

3.3.5 Cytotoxicity							107

3.4 Discussion								110

Section								        Page

4. Chapter Four:								119

‘An investigation into the uptake and intracellular fate of a series of different surface coated quantum dots in vitro’

4.1 Introduction								120

4.2 Materials and Methods						122

4.2.1 Cellular Uptake and Fate of Particles			122

4.2.1.1 Investigation to determine NP 			122

location inside endosomes

4.2.1.1.1 Fixed Cell Preparation			122

4.2.1.1.2 Immunofluorescent Staining and 	122

Imaging

4.2.1.2 Investigation to determine NP location 		123

inside lysosomes

4.2.1.3 Investigation to determine NP location 		124

inside the mitochondria

4.2.1.4 Investigation of NP uptake and intracellular 	125

fate via T.E.M.

4.2.1.4.1 Cell Preparation and Fixation		125

4.2.1.4.1.1 T.E.M. Particle Only 	126

Controls

4.2.1.4.2 Final Preparation of T.E.M. Samples   126

4.2.1.4.3 Imaging of T.E.M. Samples		127

Section								        Page

4. Chapter Four (continued):

4.2.2 Analysis of J774.A1 cell morphology and 		127

chemical content by S.E.M. and EDX Analysis

4.2.2.1 Cell Preparation and Fixation			127

4.2.2.2 Final Preparation of S.E.M. Samples		128

4.2.2.3 Imaging of S.E.M. Samples			128

4.2.2.3.1 EDX Analysis				129

4.2.2.3.2 Detection of Zn and Cd			131

4.2.3 Particle Characterisation					132

4.2.3.1 Zeta Potential					132

4.2.4 Statistical Analysis						133

4.3 Results									134

4.3.1 Uptake and Intracellular fate of Particles		134

4.3.1.1 Determination of Particle location inside 	134

endosomes

4.3.1.2 Determination of Particle location inside 	140

lysosomes

4.3.1.3 Determination of Particle location inside		145

the mitochondria

4.3.1.4 Uptake and Fate of Particles via T.E.M.		150

4.3.2 Investigation of J774.A1 cell morphology and 	157

chemical content via S.E.M. and EDX analysis

4.3.2.1. EDX Analysis following treatment with QDs	163

4.3.3 Particle Characterisation - Zeta Potential		164

4.3.3.1 Effects 10% FCS on the zeta potential 		165

of particles

Section								        Page

4. Chapter Four (continued):

4.4 Discussion								167

5. Chapter Five:								173

‘Quantum dot cytotoxicity in vitro: A comparison of the cytotoxic effects of different quantum dot surface coatings and their chemical components’

5.1 Introduction								174

5.2 Materials and Methods						176

5.2.1 Cytotoxicity							176

5.2.1.1 MTT assay 						176

5.2.1.2 LDH release						176

5.2.1.3 Cytotoxicity of QD chemical components	177

5.2.1.3.1 QD chemical components		177

5.2.2 Digital Light Microscopy of QD Chemical Components	178

5.2.3 Statistical Analysis						179

Section								        Page

5. Chapter Five (continued):

5.3 Results									180

5.3.1 Cytotoxicity							180

5.3.1.1 Validity of different MTT reagent treatment 	180

periods

5.3.1.2 QD Cytotoxicity – MTT assay			181

5.3.1.3 QD Cytotoxicity – LDH Release			185

5.3.1.4 PB Cytotoxicity					188

5.3.1.4.1 20nm PBs – MTT Assay			188

5.3.1.4.1.1 20nm PBs – MTT Assay: 	189

+ 10% FCS vs. – 10% FCS

5.3.1.4.2 20nm PBs – LDH Release	192

5.3.1.4.2.1 20nm PBs – LDH Release: 	193

+ 10% FCS vs. – 10% FCS

5.3.1.4.3 200nm PBs – MTT Assay	195

5.3.1.4.3.1 200nm PBs – 		196

MTT Assay:

+ 10% FCS vs. – 10% FCS

5.3.1.4.4 200nm PBs – LDH Release	200

5.3.1.4.4.1 200nm PBs – 		201

LDH Release:

+ 10% FCS vs.  – 10% FCS

5.3.1.4.5 20nm PBs vs. 200nm PBs	203

5.3.1.5 QD Chemical Components – MTT Assay	204

5.3.1.6 QD Chemical Component– LDH Release	209

Section								        Page

5. Chapter Five (continued):

5.3 Results (continued)

5.3.2 Effects of QD Chemical Components on 			215

J774.A1 morphology

5.4 Discussion								218

6. Chapter Six:								225

‘An investigation into the potential for different surface coated quantum dots to cause oxidative stress and affect macrophage cell signalling in vitro’

6.1 Introduction								226

6.2 Materials and Methods						228

6.2.1 Oxidative Stress						228

6.2.1.1 Measurement of Intracellular Glutathione 	228

– Cell extract preparation

6.2.1.1.1 Determination of GSH in J774.A1 	229

cell extracts

6.2.1.1.2 Determination of GSSG in J774.A1 	230

cell extracts

6.2.1.1.3 Determination of J774.A1 cell 		230

protein content

Section								        Page

6. Chapter Six (continued):

6.2 Materials and Methods (continued)

6.2.2 Ca2+ Signalling						231

6.2.2.1 Measurement of Intracellular Ca2+		231

6.2.2.1.1 Carbon black - Particle 			232

characteristics and preparation

6.2.2.2 Measurement of intracellular Ca2+ - 		233

Antioxidant pre-treatment

6.2.2.3 Measurement of resting Ca2+ - Data analysis	234

6.2.3. Pro-inflammatory Cytokine TNF-			235

6.2.5 Statistical Analysis						235

6.3 Results									236

6.3.1 Oxidative Stress 						236

6.3.1.1 GSH.Protein-1 following treatment 		236

with QDs

6.3.1.2 GSH.Protein-1 following treatment with 		239

20nm PBs

6.3.1.2.1 GSH.Protein-1 - 20nm PBs; 		239

+ 10% FCS vs. -10% FCS

6.3.1.3 GSH.Protein-1 following treatment with 		242

200nm PBs

6.3.1.3.1 GSH.Protein-1 - 200nm PBs; 		242

+10% FCS vs. -10% FCS

6.3.1.4 GSH.Protein-1 - 20nm PBs vs. 200nm PBs	246

Section								        Page

6. Chapter Six (continued):

6.3 Results (continued)

6.3.2 Intracellular Ca2+						247

6.3.2.1 Resting Cytosolic Ca2+				247

6.3.2.2 Thapsigargin response				248

6.3.2.3 Antioxidant Pre-treatment with Trolox and 	250

Na-cystelyn

6.3.3 Pro-Inflammatory Cytokine TNF-			251

6.3.3.1 Detection of TNF-production following 	251

treatment with QDs

6.3.3.2 Detection of TNF-production following 	252

treatment with PBs

6.3.3.3 Detection of TNF-production – 			253

20nm PBs vs. 200nm PBs

6.3.3.4 Detection of TNF- production – 			253

+10% FCS vs. -10% FCS

6.4 Discussion								255

7. Chapter Seven – General Discussion				263

7.1 General Discussion 						264

References									271

Appendices									298

Publications									304

Supplementary Data DVD			  Attached to back cover

FIGURES AND TABLES

Section								        Page

1. Chapter One: Introduction						1

Figure 1.1:	An example of some of the suggested consumer 	7

applications using nanotechnology.

Figure 1.2:	A simplified example of the different potential 		14

exposure routes of NPs and their subsequent fate

within the body.

Figure 1.3:	Light microscopy image of J774.A1 murine 		18

macrophage cells treated with cell culture medium

only and stained with Romanovsky staining solution.

Figure 1.4:	Example of the composition of a QD.  			34

Figure 1.5:	Example of the change in emission wavelength 	37

of QDs in proportion to their size.

2. Chapter Two: General Methods					47

Figure 2.1:	Example of the chemical structure of all QDs used.	49

Figure 2.2: 	Example of the chemical structure of each sized 	50

PB used.

3. Chapter Three:								55

‘The impact of different nanoparticle surface chemistry and size on uptake, stability and toxicity in a murine macrophage cell line’

Table 3.1: Optical parameters used for all fixed cell 			60

confocal microscopy.

Section								        Page

3. Chapter Three (continued):

Figure 3.1: Example of J774.A1 cell auto-fluorescence 		63

observed during the live cell imaging protocol in the

presence of phenol red and 10% FCS.

Table 3.2: Optical parameters used for all live cell 			64

confocal microscopy.

Figure 3.2: Example of the hydrophobic nature of organic QDs.	65

Table 3.3: Parameters used for cellular fluorescence analysis 	66

of J774.A1 cells treated with QDs and PBs via

flow cytometry.

Figure 3.3: Example of a J774.A1 cell population identified via         66

flow cytometry.

Figure 3.4a: Example geometric mean fluorescent intensity 		67

(GMFI) of J774.A1 cells following treatment with

cell culture medium only for 30 minutes.

Figure 3.4b: Example geometric mean fluorescent intensity 		67

(GMFI) of J774.A1 cells following treatment with

20nm PBs (50µg.ml-1) for 30 minutes.

Figure 3.5: Laser scanning confocal microscopy images of 		74

J774.A1 cells treated with the series of antibodies

used for cytoskeleton tubulin to determine if

non-specific antibody binding occurred during

the immunoflurescent staining technique.

Section								        Page

3. Chapter Three (continued):

Figure 3.6: Laser scanning confocal microscopy images of 		76

J774.A1 murine ‘macrophage-like’ cells after

treatment with or without Trypan blue (0.4% solution).

Figure 3.7a: Laser scanning confocal microscopy images of 		77

J774.A1 cells stained with cytoskeleton tubulin

and nuclear Hoechst following treatment with

complete medium only, COOH QDs and

NH2 (PEG) QDs (40nM) at 30, 60 and 120 minutes.

Figure 3.7b: Laser scanning confocal microscopy images of             78

J774.A1 cells stained with cytoskeleton tubulin and

nuclear Hoechst following treatment with

complete medium only, 20nm PBs and 200nm PBs

(50µg.ml-1) at 30, 60 and 120 minutes.

Figure 3.7c: Laser scanning confocal microscopy z-stack images     79

of J774.A1 cells stained with cytoskeleton tubulin and

treated with COOH QDs (40nM) at 30, 60 and

120 minutes.

Figure 3.7d: Laser scanning confocal microscopy z-stack images	  80

of J774.A1 cells stained with cytoskeleton tubulin and

treated with NH2 (PEG) QDs (40nM) at 30, 60 and

120 minutes.

Figure 3.7e: Laser scanning confocal microscopy z-stack images	   81

of J774.A1 cells stained with cytoskeleton tubulin and

treated with 20nm PBs (50µg.ml-1) at 30, 60 and

120 minutes.

Section								        Page

3. Chapter Three (continued):

Figure 3.7f: Laser scanning confocal microscopy z-stack images 	82

of J774.A1 cells stained with cytoskeleton tubulin and

treated with 200nm PBs (50µg.ml-1) at 30, 60 and

120 minutes.

Figure 3.7g: Laser scanning confocal microscopy z-stack images	   84

restored using Imaris® of J774.A1 cells stained

with cytoskeleton tubulin and treated with

COOH QDs, NH2 (PEG) QDs (both 40nM), 20nm PBs

and 200nm PBs (both 50µg.ml-1) at 30, 60 and 120 minutes.

Figure 3.7h: Laser scanning confocal microscopy z-stack 		   85

images restored using the Imaris®

co-localisation surpass module of J774.A1 cells

stained with cytoskeleton tubulin staining and

treated with COOH QDs, NH2 (PEG) QDs

(both 40nM), 20nm PBs and 200nm PBs

(both 50µg.ml-1) at 30, 60 and 120 minutes.

Figure 3.8a: Live imaging of J774.A1 cells treated with 		   87

cell culture medium only for 60 minutes.

Figure 3.8b:	Live imaging of J774.A1 cells treated with 		   88

organic QDs (40nM) for 60 minutes.

Figure 3.8c: Live imaging of J774.A1 cells treated with 		   89

COOH QDs (40nM) for 60 minutes.

Figure 3.8d: Live imaging of J774.A1 cells treated with		    90

NH2 (PEG) QDs (40nM) for 60 minutes.

Section								        Page

3. Chapter Three (continued):

Figure 3.8e: Live imaging of J774.A1 cells treated with 		92

20nm PBs (50µg.ml-1) for 60 minutes.

Figure 3.8f: Live imaging of J774.A1 cells treated with		93

200nm PBs (50µg.ml-1) for 60 minutes.

Figure 3.9a: Flow cytometry overlay histograms showing the 	 95

GMFI of J774.A1 cells following treatment with

organic QDs, COOH QDs and NH2 (PEG) QDs

(40nM) at 0, 30, 60 and 120 minutes.

Figure 3.9b: Flow cytometry overlay histograms showing		 96

the GMFI of J774.A1 cells following treatment

with 20nm PBs and 200nm PBs (50µg.ml-1)

at 0, 30, 60 and 120 minutes.

Figure 3.10a: Relative fluorescent intensity of organic, COOH 	 99

and NH2 (PEG) QDs (40nM) at pH 4.0 over

120 minutes at a slit-width of 7nm.

Figure 3.10b: Relative fluorescent intensity of organic, COOH	 99

and NH2 (PEG) QDs (40nM) at pH 7.0 over

120 minutes at a slit-width of 7nm.

Figure 3.10c: Relative fluorescent intensity of COOH and 		 100

NH2 (PEG) QDs (40nM) at pH 4.0 over 120 minutes

at a slit-width of 15nm.

Figure 3.10d: Relative fluorescent intensity of COOH and 		 100

NH2 (PEG) QDs (40nM) at pH 7.0 over 120 minutes

at a slit-width of 15nm.

Section								        Page

3. Chapter Three (continued):

Figure 3.10e: Relative fluorescent intensity of 20nm and 		101

200nm PBs (50μg.ml-1) at pH 4.0 over 120 minutes

at a slit-width of 12nm.

Figure 3.10f: Relative fluorescent intensity of 20nm and 		 101

200nm PBs (50μg.ml-1) at pH 7.0 over 120 minutes

at a slit-width of 12nm.

Table 3.4: Changes in mean NP Ø (nm) of organic, 			  102

COOH, and NH2 (PEG) QDs (all 40nM), as well as

20nm and 200nm PBs (both 50µg.ml-1), as determined

by DLS over a 30 minute period in cell-free culture

medium at pH 4.0.

Figure 3.11a: Relative fluorescent intensity at slit-width 15nm 	   104

of complete cell culture medium from J774.A1 cells

after (i) treatment with organic, COOH or

NH2 (PEG) QDs (40nM) for 30 minutes, and

(ii) washing to remove extracellular QDs prior to

a further 120 minute incubation period.

Figure 3.11b: Relative fluorescent intensity at slit-width 12nm 	    104

of complete cell culture medium from J774.A1 cells

after (i) treatment with 20nm or 200nm PBs

(50μg.ml-1) for 30 minutes, and (ii) washing to

remove extracellular PBs prior to a further

120 minute incubation period.

Section								        Page

3. Chapter Three (continued):

Figure 3.12a: Exocytosis adsorption control for organic, COOH 	105

and NH2 (PEG) QDs (40nM) after 0 and 30 minutes

at a slit-width of 15nm in the presence of J774.A1

cells.

Figure 3.12b: Exocytosis adsorption control for organic, COOH  	105

and NH2 (PEG) QDs (40nM) after 0 and 30 minutes

at a slit-width of 15nm in the absence of J774.A1

cells.

Figure 3.12c: Exocytosis adsorption control for 20nm or 		106

200nm PBs (50μg.ml-1) after 0 and 30 minutes

at a slit-width of 12nm in the presence of J774.A1

cells.

Figure 3.12d: Exocytosis adsorption control for 20nm and	106

200nm PBs (50μg.ml-1) after 0 and 30 minutes

at a slit-width of 12nm in the absence of J774.A1

cells.

Figure 3.13: The effects of organic, COOH and NH2 (PEG) QDs      107

(all 40nM), as well as 20nm and 200nm PBs

(both 50µg.ml-1) on the mitochondrial metabolic

activity (MTT assay) of J774.A1 cells at two hours.

Figure 3.14a: Percentage LDH release from J774.A1 cells 	108

following treatment with organic, COOH and

NH2 (PEG) QDs (40nM) over a two hour period.

Section								        Page

3. Chapter Three (continued):

Figure 3.14b: Percentage LDH release from J774.A1 cells 		108

following treatment with 20nm and 200nm PBs

(50µg.ml-1) over a two hour period.

Figure 3.15a: LDH release from J774.A1 cells following a 		109

one hour incubation of either organic, COOH

or NH2 (PEG) QDs (40nM) with a lysed extract

of J774.A1 cells.

Figure 3.15b: LDH release from J774.A1 cells following a 		109

one hour incubation of either 20nm or

200nm PBs (both 50µg.ml-1) with a lysed extract

of J774.A1 cells.

4. Chapter Four:								119

‘An investigation into the uptake and intracellular fate of a series of different surface coated quantum dots in vitro’

Table 4.1: Optical parameters used for confocal microscopy 		123

of J774.A1cells stained with EEA-1.

Table 4.2: Optical parameters used for confocal microscopy 		124

of J774.A1cells stained with Lysotracker®.

Table 4.3: Optical parameters used for confocal microscopy 		125

of J774.A1cells stained with Mitotracker®.

Figure 4.1a: An example of an S.E.M. image of a J774.A1 cell 	130

treated with organic QDs (40nM) for 24 hours,

prepared for EDX analysis at a 4000x magnification.

Section								        Page

4. Chapter Four (continued):

Figure 4.1b: An example of a sum spectrum output from 		130

the INCA microanalysis suite following EDX

analysis of J774.A1 cells treated with organic QDs

(40nM) for 24 hours.

Figure 4.2a: An example of a sum spectrum output highlighting 	131

cadmium from the INCA microanalysis suite following

EDX analysis of J774.A1 cells treated with organic QDs

(40nM) for 24 hours.

Figure 4.2b: An example of a sum spectrum output highlighting 	132

zinc from the INCA microanalysis suite following

EDX analysis of J774.A1 cells treated with organic QDs

(40nM) for 24 hours.

Figure 4.3: Laser scanning confocal microscopy images of 		134

J774.A1 cells treated with the series of antibodies

used to detect EEA-1 to determine if

non-specific antibody binding occurred during

the immunoflurescent staining technique.

Figure 4.4a:  Laser scanning confocal microscopy images 		136

of J774.A1 cells stained with an Ab to detect

EEA-1 and treated with complete medium only

for, 10, 30, 60 minutes and 120 minutes.

Figure 4.4b: Laser scanning confocal microscopy images 		137

of J774.A1 cells stained with an Ab to detect

EEA-1 and treated with COOH QDs or

NH2 (PEG) QDs at 40nM for

10, 30, 60 and 120 minutes.

Section								        Page

4. Chapter Four (continued):

Figure 4.4c: Laser scanning confocal microscopy images		139

of J774.A1 cells stained with an Ab to detect

EEA-1 and treated with 20nm or 200nn PBs

at 50μg.ml-1 for 10, 30, 60 and 120 minutes.

Figure 4.5a: Laser scanning confocal microscopy images 		140

of J774.A1 cells stained with Lysotracker® (50µM)

and treated with complete medium only for

0, 10, 30, 60 and 120 minutes.

Figure 4.5b: Laser scanning confocal microscopy images 		142

of J774.A1 cells stained with Lysotracker® (50µM)

and treated with COOH QDs or NH2 (PEG) QDs

at 40nM for 10, 30, 60 and 120 minutes.

Figure 4.5c: Laser scanning confocal microscopy images		144

of J774.A1 cells stained with Lysotracker® (50µM)

and treated with 20nm or 200nn PBs at 50μg.ml-1

for 10, 30, 60 and 120 minutes.

Figure 4.6a: Laser scanning confocal microscopy images 		145

of J774.A1 cells stained with the cell permeable

antibody Mitotracker® (500µM) and treated with

complete medium only for 0, 10, 30, 60 and

120 minutes.

Figure 4.6b: Laser scanning confocal microscopy images		147

of J774.A1 cells stained with the cell permeable

antibody Mitotracker® (500µM) and treated with

COOH QDs or NH2 (PEG) QDs at 40nM for

10, 30, 60 and 120 minutes.

Section								        Page

4. Chapter Four (continued):

Figure 4.6c: Laser scanning confocal microscopy images 		149

of J774.A1 cells stained with the cell permeable

antibody Mitotracker® (500µM) and treated with

20nm or 200nm PBs at 50µg.ml-1 for

10, 30, 60 and 120 minutes.

Figure 4.7a: Transmission electron microscopy (T.E.M.) 		150

image of organic QD (40nM) particle only control.

Figure 4.7b: Transmission electron microscopy (T.E.M.) 		151

image of COOH QD and NH2 (PEG) QD (40nM)

particle only controls.

Figure 4.7c: Transmission electron microscopy (T.E.M.) 		152

image of 20nm PB and 200nm PB (50µg.ml-1)

particle only controls.

Figure 4.7d: Transmission electron microscopy (T.E.M.) 		154

images of J774.A1 cells treated with complete

medium only and organic QDs (40nM) at two hours.

Figure 4.7e: Transmission electron microscopy (T.E.M.)		155

images of J774.A1 cells treated with COOH QDs

and NH2 (PEG) QDs (40nM) at two hours.

Figure 4.7f: Transmission electron microscopy (T.E.M.) 		156

images of J774.A1 cells treated with 20nm PBs and

200nm PBs (50µg.ml-1) at two hours.

Section								        Page

4. Chapter Four (continued):

Figure 4.8a: Scanning electron microscopy (S.E.M.) images 		158

of J774.A1 cells treated with complete medium only,

organic QDs, COOH QDs and NH2 (PEG) QDs (40nM)

at 30 minutes.

Figure 4.8b: Scanning electron microscopy (S.E.M.) images 	159

of J774.A1 cells treated with complete medium only,

20nm PBs and 200nm PBs (50µg.ml-1) at 30 minutes.

Figure 4.8c: Scanning electron microscopy (S.E.M.) images 		160

of J774.A1 cells treated with complete medium only,

organic QDs, COOH QDs and NH2 (PEG) QDs

(40nM) at two hours.

Figure 4.8d: Scanning electron microscopy (S.E.M.) images 	161

of J774.A1 cells treated with complete medium only,

20nm PBs and 200nm PBs (50µg.ml-1) at two hours.

Figure 4.8e: Scanning electron microscopy (S.E.M.) images		162

of J774.A1 cells treated with complete medium only,

organic QDs, COOH QDs and NH2 (PEG) QDs (40nM)

at 24 hours.

Figure 4.8f: Scanning electron microscopy (S.E.M.) images	163

of J774.A1 cells treated with complete medium only

20nm PBs and 200nm PBs (50µg.ml-1) at 24 hours.

Section								        Page

4. Chapter Four (continued):

Table 4.4a:  Changes in the mean zeta potential (mV) of 		165

organic, COOH and NH2 (PEG) QDs (40nM),

as well as both 20nm and 200nmPBs (50µg.ml-1)

at pH 4.0 in the presence of 10% FCS.

Table 4.4b: Changes in the mean zeta potential (mV) of 		166

organic, COOH and NH2 (PEG) QDs (40nM),

as well as both 20nm and 200nmPBs (50µg.ml-1)

at pH 4.0 in the absence of 10% FCS.

5. Chapter Five:								173

‘Quantum dot cytotoxicity in vitro: A comparison of the cytotoxic effects of different quantum dot surface coatings and their chemical components’

Figure 5.1a: MTT absorbance of J774.A1 cells treated		180

with either complete medium only or

20nm PBs (50µg.ml-1) in the presence of

10% FCS at two hours.

Section								        Page

5. Chapter Five (continued):

Figure 5.1b: MTT absorbance of J774.A1 cells treated 		181

with either complete medium only or

20nm PBs (50µg.ml-1) in the absence of

10% FCS at two hours.

Figure 5.2a: The effects of organic, COOH and NH2 (PEG) QDs 	182

(20, 40 and 80nM) on the metabolic activity

(MTT assay) of J774.A1 cells at two hours.

Figure 5.2b: The effects of organic, COOH and NH2 (PEG) QDs 	183

(20, 40 and 80nM) on the metabolic activity

(MTT assay) of J774.A1 cells at four hours.

Figure 5.2c: The effects of organic, COOH and NH2 (PEG) QDs 	184

(20, 40 and 80nM) on the metabolic activity

(MTT assay) of J774.A1 cells at 24 hours.

Figure 5.2d: The effects of organic, COOH and NH2 (PEG) QDs 	185

(20, 40 and 80nM) on the metabolic activity

(MTT assay) of J774.A1 cells at 48 hours.

Figure 5.3a: Percentage LDH release from J774.A1 cells 		186

treated with organic, COOH and NH2 (PEG) QDs

(20, 40 and 80nM) at two hours.

Figure 5.3b: Percentage LDH release from J774.A1 cells 		187

treated with organic, COOH and NH2 (PEG) QDs

(20, 40 and 80nM) at four hours.

Section								        Page

5. Chapter Five (continued):

Figure 5.3c: Percentage LDH release from J774.A1 cells 		187

treated with organic, COOH and NH2 (PEG) QDs

(20, 40 and 80nM) at 24 hours.

Figure 5.3d: Percentage LDH release from J774.A1 cells 		188

treated with organic, COOH and NH2 (PEG) QDs

(20,40 and 80nM) at 48 hours.

Figure 5.4a: The effects of 20nm PBs (12.5-100µg.ml-1) 		189

either in the presence or absence of 10% FCS

on the metabolic activity (MTT assay) of

J774.A1 cells at two hours.

Figure 5.4b: The effects of 20nm PBs (12.5-100µg.ml-1) 		190

either in the presence or absence of 10% FCS

on the metabolic activity (MTT assay) of

J774.A1 cells at four hours.

Figure 5.4c: The effects of 20nm PBs (12.5-100µg.ml-1) 		191

either in the presence or absence of 10% FCS

on the metabolic activity (MTT assay) of

J774.A1 cells at 24 hours.

Figure 5.4d: The effects of 20nm PBs (12.5-100µg.ml-1) 		192

either in the presence or absence of 10% FCS

on the metabolic activity (MTT assay) of

J774.A1 cells at 48 hours.

Figure 5.5a: Percentage LDH release from J774.A1 cells treated 	193

with 20nm PBs (12.5-100µg.ml-1) either in the

presence or absence of 10% FCS at two hours.

Section								        Page

5. Chapter Five (continued):

Figure 5.5b: Percentage LDH release from J774.A1 cells treated 	194

with 20nm PBs (12.5-100µg.ml-1) either in the

presence or absence of 10% FCS at four hours.

Figure 5.5c: Percentage LDH release from J774.A1 cells treated 	194

with 20nm PBs (12.5-100µg.ml-1) either in the

presence or absence of 10% FCS at 24 hours.

Figure 5.5d: Percentage LDH release from J774.A1 cells 		195

treated with 20nm PBs (12.5-100µg.ml-1) either

in the presence or absence of 10% FCS at

48 hours.

Figure 5.6a: The effects of 200nm PBs (12.5-100µg.ml-1) 		197

either in the presence or absence of 10% FCS

on the metabolic activity (MTT assay) of

J774.A1 cells at two hours.

Figure 5.6b: The effects of 200nm PBs (12.5-100µg.ml-1) 		198

either in the presence or absence of 10% FCS

on the metabolic activity (MTT assay) of

J774.A1 cells at four hours.

Figure 5.6c: The effects of 200nm PBs (12.5-100µg.ml-1) 		199

either in the presence or absence of 10% FCS

on the metabolic activity (MTT assay) of

J774.A1 cells at 24 hours.

Section								        Page

5. Chapter Five (continued):

Figure 5.6d: The effects of 200nm PBs (12.5-100µg.ml-1) 		200

either in the presence or absence of 10% FCS

on the metabolic activity (MTT assay) of

J774.A1 cells after 48 hours.

Figure 5.7a: Percentage LDH release from J774.A1 cells 		201

treated with 200nm PBs (12.5-100µg.ml-1) either

in the presence or absence of 10% FCS at

two hours.

Figure 5.7b: Percentage LDH release from J774.A1 cells 		202

treated with 200nm PBs (12.5-100µg.ml-1) either

in the presence or absence of 10% FCS at

four hours.

Figure 5.7c: Percentage LDH release from J774.A1 cells 		202

treated with 200nm PBs (12.5-100µg.ml-1) either

in the presence or absence of 10% FCS at

24 hours.

Figure 5.7d: Percentage LDH release from J774.A1 cells 		203

treated with 200nm PBs (12.5-100µg.ml-1) either

in the presence or absence of 10% FCS at

48 hours.

Figure 5.8a: The effects of QD chemical components; 		206

organic solvent vehicle mixture (O.S.), ZnS and

CdCl2; at 20, 40 and 80nM on the metabolic activity

(MTT assay) of  J774.A1 cells at two hours.

Section								        Page

5. Chapter Five (continued):

Figure 5.8b: The effects of QD chemical components; 		207

organic solvent vehicle mixture (O.S.), ZnS and

CdCl2; at 20, 40 and 80nM on the metabolic activity

(MTT assay) of J774.A1 cells at four hours.

Figure 5.8c: The effects of QD chemical components; 		208

organic solvent vehicle mixture (O.S.), ZnS and

CdCl2; at 20, 40 and 80nM on the metabolic activity

(MTT assay) of J774.A1 cells at 24 hours.

Figure 5.8d: The effects of QD chemical components; 		209

organic solvent vehicle mixture (O.S.), ZnS and

CdCl2; at 20, 40 and 80nM on the metabolic

activity (MTT assay) of J774.A1 cells at 48 hours.

Figure 5.9a: Percentage LDH release from J774.A1 cells 		211

following treatment with QD chemical components;

organic solvent vehicle mixture (O.S.), ZnS

and CdCl2; at 20, 40 and 80nM at two hours.

Figure 5.9b: Percentage LDH release from J774.A1 cells 		212

following treatment with QD chemical components;

organic solvent vehicle mixture (O.S.), ZnS

and CdCl2; at 20, 40 and 80nM at four hours.

Figure 5.9c: Percentage LDH release from J774.A1 cells 		213

following treatment with QD chemical components;

organic solvent vehicle mixture (O.S.), ZnS

and CdCl2; at 20, 40 and 80nM at 24 hours.

Section								        Page

5. Chapter Five (continued):

Figure 5.9d: Percentage LDH release from J774.A1 cells 		214

following treatment with QD chemical components;

organic solvent vehicle mixture (O.S.), ZnS

and CdCl2; at 20, 40 and 80nM at 48 hours.

Figure 5.10: Light microscopy images of J774.A1 cells treated 	216

with QD chemical components; organic solvent

vehicle mixture (O.S.), ZnS and CdCl2; at 40nM

at 2 hours and stained with Romanovski staining

solution.

Figure 5.11: Rate of ZnS precipitation in complete medium 		217

over 2 hours.

6. Chapter Six:								225

‘An investigation into the potential for different surface coated quantum dots to cause oxidative stress and affect macrophage cell signalling in vitro’

Figure 6.1: Example fluorimeter trace reading of J774.A1 		233

cytosolic Ca2+ following treatment with organic QDs

(40nM), as determined via the use of the fluorescent

calcium chelator Fura 2-AM.

Figure 6.2a: GSH.protein-1 levels in J774.A1 cell extracts 		237

after treatment with organic, COOH and

NH2 (PEG) QDs for two hours.

Section								        Page

6. Chapter Six (continued):

Figure 6.2b: GSH.protein-1 levels in J774.A1 cell extracts 		237

after treatment with organic, COOH and

NH2 (PEG) QDs for four hours.

Figure 6.2c: GSH.protein-1 levels in J774.A1 cell extracts 		238

after treatment with organic, COOH and

NH2 (PEG) QDs for six hours.

Figure 6.2d: GSH.protein-1 levels in J774.A1 cell extracts 		238

after treatment with organic, COOH and

NH2 (PEG) QDs for 24 hours.

Figure 6.3a:  GSH.protein-1 levels in J774.A1 cell extracts 		240

after treatment with 20nm PBs either in the

presence or absence of 10% FCS for two hours.

Figure 6.3b: GSH.protein-1 levels in J774.A1 cell extracts 		240

after treatment with 20nm PBs either in the

presence or absence of 10% FCS for four hours.

Figure 6.3c: GSH.protein-1 levels in J774.A1 cell extracts 		241

after treatment with 20nm PBs either in the

presence or absence of 10% FCS for six hours.

Figure 6.3d: GSH.protein-1 levels in J774.A1 cell extracts 		241

after treatment with 20nm PBs either in the

presence or absence of 10% FCS for 24 hours.

Figure 6.4a: GSH.protein-1 content in J774.A1 cell extracts 		243

after treatment with 200nm PBs either in the

presence or absence of 10% FCS for two hours.

Section								        Page

6. Chapter Six (continued):

Figure 6.4b: GSH.protein-1 content in J774.A1 cell extracts		244

after treatment with 200nm PBs either in the

presence or absence of 10% FCS for four hours.

Figure 6.4c: GSH.protein-1 content in J774.A1 cell extracts		245

after treatment with 200nm PBs either in the

presence or absence of 10% FCS for six hours.

Figure 6.4d: GSH.protein-1 content in J774.A1 cell extracts 		246

after treatment with 200nm PBs either in the

presence or absence of 10% FCS for 24 hours.

Figure 6.5a: Cytosolic Ca2+ concentration (nM) of J774.A1 cells 	247

following treatment with organic, COOH and

NH2 (PEG) QDs for 30 minutes.

Figure 6.5b: Cytosolic Ca2+ concentration (nM) of J774.A1 cells 	248

following treatment with 20nm PBs, 200nm PBs,

ufCB and CB for 30 minutes.

Figure 6.6a: Thapsigargan response of J774.A1 cells following 	249

treatment with organic, COOH and NH2 (PEG) QDs

for 30 minutes.

Figure 6.6b: Thapsigargan response of J774.A1 cells following 	249

treatment with 20nm PBs, 200nm PBs, ufCB and CB

for 30 minutes.

Section								        Page

6. Chapter Six (continued):

Figure 6.7a: Cytosolic Ca2+ concentration of cells treated with 	250

the antioxidant TROLOX (25µM) for 30 minutes

prior to treatment with organic COOH and

NH2 (PEG) QDs for an additional 30 minutes.

Figure 6.7b: Cytosolic Ca2+ concentration of cells treated with 	251

the antioxidant Na-cystelyn (400µM) for 30 minutes

prior to treatment with organic COOH and

NH2 (PEG) QDs for an additional 30 minutes.

Figure 6.8: Stimulation of the pro-inflammatory cytokine TNF- 	252

detected in J774.A1 cell supernatants after treatment

with organic, COOH and NH2 (PEG) QDs at 24 hours.

Figure 6.9a: Stimulation of the pro-inflammatory cytokine TNF- 	253

detected in J774.A1 cell supernatants after treatment

with 20nm PBs either in the presence or absence of

10% FCS at 24 hours.

Figure 6.9b: Stimulation of the pro-inflammatory cytokine TNF- 	254

detected in J774.A1 cell supernatants after treatment

with 200nm PBs either in the presence or absence of

10% FCS at 24 hours.

APPENDICES

Appendix								        Page

Appendix One: 	Standard solutions used for assessment of	299

lactate dehydrogenase (LDH) activity in

particulate treated J774.A1 cells

Appendix Two: 	The ‘Smoluchowski’ Equation			300

Appendix Three: 	Standard solutions used for assessment of	301

reduced glutathione (GSH) levels in

particulate treated J774.A1 cells

Appendix Four: 	Standard solutions used for assessment of 	302

oxidised glutathione (GSSG) levels in

particulate treated J774.A1 cells

Appendix Five:   	Standard solutions used for assessment of 	303

cellular protein levels in particulate

treated J774.A1 cells

LIST OF ABBREVIATIONS

(in alphabetical order)

Ab 			- Antibody

AM 			- Acetoxy methyl

ANOVA 		- Analysis of Variance

AOT			- Sodium dioctyl sulfosuccinate

AP-1			- Activator protein-1

ATP 			- Adenosine 5’-triphosphate

Au			- Gold

BAL 			- Bronchoalveolar Lavage

BALB/c		- An albino strain of laboratory mouse

BEAS-2B cells	- Human bronchial epithelial cell-line

BSA 			- Bovine Serum Albumin

BSI			- British Standards Institute

C			- Carbon

13C			- Carbon-13

Ca2+			- Calcium

CB 			- Carbon Black

Cd			- Cadmium

Cd2+ 			- Cadmium ions

CdCl2			- Cadmium Chloride

CdSe 			- Cadmium Selenide

CdTe 			- Cadmium Telluride

cm2			- squared centimetre

CME			- Clathrin-mediated endocytosis

CNS 			- Central Nervous System

CNTs			- Carbon nanotubes

COOH 		- Carboxylate

COPD 		- Chronic Obstructive Pulmonary Disease

CPC			- Cetylpyridinium chloride

CST			- Council for Science and Technology

CV system		- Cardiovascular system

C3H3NaO3		- Sodium pyruvate

DCFH			- 2',7'-dichlorofluorescin

DCFH-7		- 2',7'-dichlorofluorescin-7

DCFH-DA		- 2’,7’-dichlorofluorescin-diacetate

DEFRA 		- Department for Environment, Food and Rural Affairs

DEP			- Diesel exhaust particles

DHE 			- Dihydroethidium

DLS 			- Dynamic Light Scattering

DMEM 		- Dulbecco’s Modified Eagle’s Medium

DMSO 		- Dimethyl sulfoxide

DM1A			- Purified Mouse clone Immunoglobulin

DNA			- Deoxyribose nucleic acid

DPX			- Distyrene di-n-butylphthalate xylene

DTT			- Dithiothreitol

ECACC 		- European collection of cell cultures

EDTA 		- Tetra ethylene diamine tetraacetic acid

EDX 			- Energy Dispersive X-ray

EEA-1 		- Early Endocytic antigen-1

EELS			- Electron energy loss spectroscopy

EFTEM 		- Energy Filtering Transmissaion Electron Microscopy

EGTA 		- Ethylene glycol tetraacetic acid

EL-4 cells		- Mouse lymphoma cell-line

ELISA 		- Enzyme linked immunosorbant assay

EMEM 		- Eagle’s minimum essential medium

ER 			- Endoplasmic Reticulum

ESF 			- European Science Foundation

F-68 CTAB		- Block Co-polymer/surfactant (F-68) Cetyltrimethyl

ammonium bromide

FBS 			- Foetal bovine serum

FCS 			- Foetal calf serum

Fe			- Iron

FeCl2			- Iron Chloride

FEG-SEM 		- Field Emission Gun Scanning Electron Microscope

FL-1 (Flow Cytometry) -	Detector Filter Laser 1 (530nm ± 30nm)

FL-2 (Flow Cytometry) - Detector Filter Laser 2 (585nm ± 30nm)

FSC 			- Forward scatter mode (Flow Cytometry)

GI 			- Gastrointestinal tract

GMFI 			- Geometric mean fluorescent intensity

GSH 			- Reduced Glutathione

GSSG 		- Oxidised Glutathione

GTPases		- Guanine nucleotide ases

H			- Hydrogen

HCl 			- Hydrochloric acid

Hela cells		- Immortal cell-line, derived from cervical cancer cells

HeNe 			- Helium-Neon laser

HepG2 cells		- Human hepatocellular carcinoma cell-line

HEPES		- 4-(2-hydroxyethyl)-1-piperazineethanesulfonic acid

HO-1 			- Heme-oxygenase -1

HSF-42 cells		- human skin fibroblast cell-line

i.v. 			- Intercostal vein

ICP-MS 		- Inductively coupled plasma mass spectroscopy

IgG 			- Immunoglobin G

IL			- Interleukin

IL-1β			- Interleukin-1Beta

IL-6 			- Interleukin-6

IL-8 			- Interleukin-8

IMR-32 cells		- Human neuroblastoma cell-line

IMR-90 cells		- Human lung fibroblast cell-line

192Ir			- Iridium-192

J774.A1 cells	- Murine ‘macrophage-like’ cell-line

keV 			- kilo electron Volts

KHCO3 		- Potassium Bicarbonate

KOH 			- Potassium Hydroxide

LDH 			- Lactate dehydrogenase

L-G 			- L-Glutamine

m			- metre

m2			- squared metre

MCF-7 cells		- Human epithelial breast adenocarcinoma cell-line

MDA-MB-231 cells	- Breast cancer cell-line

MIP-2			- Macrophage Inflammatory Protein-2

MM6 cells		- Monomac 6 human macrophage cell-line

MPA 			- Mercaptopropianic Acid

MTT			- 3-(4,5-dimethylthiazol-2-yl)-2,5-diphenyl tetrazolium

bromide

MUA 			- Mercaptoundecanoic acid

mV 			- milliVolts

M1			- Electronic Marker 1 (Flow Cytometry)

M2			- Electronic Marker 2 (Flow Cytometry)

n			- number of ethylene glycol subunits (PEG)

N.A. 			- Numerical aperture

N9 cells		- Microglial cell-line

NAC 			- N-acetyl-L-cysteine

NAD+ 			- Nicotinamide adenine dinucleotide

NADH 		- Nicotinamide adenine nucleotide

NADPH oxidase	- nicotinamide adenine dinucleotide phosphate-

oxidase

Na2B4O7·10H2O 	- Sodium borate

NaH2PO4.2H20 	- Sodium dihydrogen orthophosphate

NaOH 		- Sodium Hydroxide

ND 			- Not detectable

NEM 			- N-ethyl maleimide

NF-κB			- Nuclear factor-kappa B

NH2 			- Amino

nm 			- Nanometre

nM			- nanoMolar

NP 			- Nanoparticle

NPs			- Nanoparticles

O			- Oxygen

O.S. 			- Organic Solvent Vehicle Mixture

OD 			- Optical Density

OPT 			- Ophthaldehyde

P/S 			- Penicillin/Streptomycin

PB 			- Polystyrene Bead

PBs 			- Polystyrene Beads

PBS 			- Phosphate buffered saline

PC12 cells		- Neuronal cell-line derived from the

pheochromocytoma of a rat adrenal medulla

PEF 			- Peak Expiratory Flow

PEG 			- Polyethylene glycol

PEI 			- Polyethylenimine

PI 			- Propidium Iodide

PM			- Particulate Matter

PMNs			- Polymorphonuclear leukocytes

PM10 			- Particulate Matter of <10µm

POC-R		- Aliuminium, black anodised perfusion, open and

closed cultivation chamber system

PTFE 			- Polytetrafluoroethylene

QD 			- Quantum dot

QDs 			- Quantum dots

RAW 264.7 cells	- Macrophage-like, Abelson leukemia virus cell-line

ROS 			- Reactive oxygen species

RPMI 			- Roswell Park Memorial Institute

SCENIHR 		- Scientific Committee on Emerging and Newly

Identified Health Risks

SDS			- Sodium Dodecyl Sulfate

S.E.M. 		- Scanning electron microscope/microscopy

SEM 			- Standard Error of the Mean

SPCM 		- Single photon counting module

SPIONs 		- Superparamagnetic iron oxide nanoparticles

SSA			- Sheep serum albumin

SSC 			- Side Scatter Mode (Flow cytometry)

SWCNTs 		- Single walled Carbon Nanotubes

T.E.M. 		- Transmission electron microscope/microscopy

TiO2 			- Titanium dioxide

TNF- 		- Tumour necrosis factor-alpha

TOP 			- Trioctyll phosphine

TOPO 		- Trioctyll phosphine oxide

Uf			- Ultrafine

ufCB 			- Ultrafine carbon black

Vero cells		- African green monkey’s kidney cells

WD 			- Working Distance

WHO EHC		- World Health Organisation Environmental Health

Criteria

ZnS 			- Zinc Sulphide

Ø			- Diameter

>			- greater than

≥			- greater than or equal to

<			- less than

≤			- less than or equal to

µ			- micro

µg			- microgram

µm			- micrometre

µM			- microMolar

λ			- wavelength

ζ			- Zeta Potential

PUBLICATIONS

Sections of this thesis have either been published, or are accepted for publication, as (i) original articles, (ii) review articles, (iii) book chapters or       (iv) abstracts. Please find a list of these publications below.

Original articles

Clift, M. J. D., Rothen-Rutishauser, B., Brown, D. M., Duffin, R., Donaldson, K., Proudfoot, L., Guy, K., and Stone, V., (2008). The Impact of Different Nanoparticle Surface Chemistry and Size on Uptake and Toxicity in a Murine Macrophage Cell Line, Toxicology and Applied Pharmacology. Accepted manuscript (Uncorrected Proof).

Review articles

Stone, V. Johnston, H. and Clift, M. J. D., (2007). Air Pollution, Ultrafine and Nanoparticle Toxicology: Cellular and Molecular Interactions,               IEEE Transactions on Nanobioscience. 6 (4), pp. 331 – 340.

Book chapters

Stone, V., Kinloch, I., Clift, M., Fernandes, T., Ford, A., Christofi, N., Griffiths, A., and Donaldson, K., (2007). Nanoparticle Toxicology and Ecotoxicology: The Role of Oxidative Stress; pp. 281 – 296.  Edited by: Zhao, Y. and Nalwa, H. S. In: Nanotoxicology; Interactions of Nanomaterials with Biological Systems; California, USA; American Scientific Publishers (ASP).

Abstracts

Wilson, M. R., Clift, M., Barlow, P., Hutchison, G., Guy, K., Griffiths, A., Simpson, R., Sales, J. and Stone, V., (2006). Pro-inflammatory and toxicological effects of zinc and nanoparticle interactions are induced via non-oxidative mechanisms, Toxicology. 219, pp. 237.

Supplementary Data DVD

Please find a supplementary data DVD located inside the back cover of this PhD thesis.

Contained on the DVD are data sets corresponding with results presented in chapter three.  The specific data sets on the DVD are;

- Figure 3.1 - Example of cell auto-fluorescence - live imaging movie1

- Figure 3.7 c-f - All confocal z-stack images2

- Figure 3.7g - All IMARIS® 3D image restoration movies1

- Figure 3.8 a-f - All live imaging movies1

1 All images can be viewed through Microsoft Windows Media Player®

2 In order to view the confocal z-stack images, it is necessary to download the LSM 5 image browser software (also located on the data DVD). This programme contains no viruses and is safe to download onto any computer which has a current version of Microsoft Windows®                         (2000 (Millenium)®, XP®, Vista®). To install this imaging software onto any computer, follow the procedure described below.

- Click on folder entitled LSM 5 image browser software

- Click on folder entitled LSM 5 image browser

- Click on folder entitled image browser

- Click on icon entitled ‘INST_IB’

- Please then follow the steps and prompts from the computer to complete installation of this software.

ACKNOWLEDGEMENTS

Over the past three years I have been very fortunate to have received an endless source of guidance and encouragement from my supervisors, peers and collaborators, without which this research project would not have been completed and to whom, therefore, I would like to express my deepest gratitude.

To my Director of Studies, Professor Vicki Stone for her invaluable assistance and support; to Dr. David M. Brown, Dr. Keith Guy and           Dr. Lorna Proudfoot for their help and advice and to Dr. Paula Smith and Dr. Arthur Robinson for their endless support throughout.

Thanks are due also to my many collaborators, including Dr. Barbara Rothen-Rutishauser (University of Bern), Professor Ken Donaldson,        Dr. Rodger Duffin, Mr. Stephen Mitchell (all University of Edinburgh),             Mr. Alan Davidson, Mr. Bill Brownlee, Mr. Matthew S. P. Boyles and              Dr. Sourav Bhattacharjee (M.D.) (all Edinburgh Napier University) Mr. Gerard Byrne (University of Nottingham), for all they have done for me.

I would also like to acknowledge the members of the biomedicine and sport science research group (BSSRG) at Edinburgh Napier University for their constant support and advice; particularly Miss Helinor Johnston            (PhD student) as well as all the research/PhD students, both past and present, within the school of life sciences at Edinburgh Napier University, whom I have had the pleasure to meet and work with.

Thanks are due to Mrs. Linda Wood and Mr. Chris Edmans for all their administrative help over the past three years; also to the administrative staff in the offices of the School of Life Sciences, the Faculty of Health, Life and Social Sciences and the Research/Graduate Schools.

I would further like to acknowledge the extensive funding received from Edinburgh Napier University and the Colt Foundation, without which this research project would not have been completed. My deepest thanks go to the British Association for Lung Research (BALR), the Engineering and Physical Sciences Research Council (EPSRC), the American Air Force Office of Scientific Research (AAFOSR), the Scottish International Education Trust (SIET), and the Carnegie Trust, all of whom provided funding for conferences, research meetings and collaborations as well as summer schools, which enabled me to present and discuss my research throughout the scientific community.

Despite the endless encouragement from my academic supervisors and peers, I would have not been able to complete this project without the constant support and guidance of my family and friends.

To my parents, David and Mary, my brother Stuart and his fiancé Selina, as well as my life long friend Craig, I give my deepest thanks for their continual support, encouragement and advice.  To my girlfriend, Kirsten, considerate throughout, the kindest, most genuine and thoughtful lady I have had the pleasure to meet, I give my deepest and most sincere thanks for everything.